MICHIGAN

DEPARTMENT OF TRANSPORTATION

SPECIAL PROVISION

FOR

DECORATIVE CONCRETE SIDEWALK

CFS:TES	1 of 4	APPR:CRB:JN:10-02-23

a.	Description.  This work consists of constructing decorative PCC sidewalk at the locations specified on the plans.  Use a Slate Grey (P9110) Integral Color with Light Gray (Brickform 600) Color Hardener and Dark Gray Release Agent using the Ashlar (TM-100) stamp pattern, with a Dolphin (P9120) Integral Color with Medium Gray (Brickform 200) Color Hardener and Dark Gray Color Release Soldier Course Used Brick (FM-5300) stamp pattern border, as shown on the plans.  Complete this work in accordance with the standard specifications, except as modified herein.

b.	Submittals.  Submit a plan showing the types and locations of joints, reinforcement, and sequence of construction.  Submit a report detailing the concrete mix designs to be used, including manufacturers and/or suppliers of mixture components.  Submit technical data sheets for a single manufacturer’s complete system for products and/or materials including admixtures, colorants, curing compounds, decorative concrete sealer, dry-shake finish materials, imprinting tools, and any other products requested by the Engineer.  Submit Test Data Certification with test results conducted by an independent testing laboratory within the past 24 months reporting that the coloring pigment conforms to the general requirements of ASTM C979/C979M.  Obtain approval from the Engineer prior to beginning work.

c.	Certification.  Furnish proof of Michigan Concrete Association (MCA) Decorative Concrete Certification, or proven equivalent manufacturer training and certification for placing decorative concrete, to the Engineer.

d.	Materials.  Use a single manufacturer’s complete system for products and/or materials.

1.	Concrete Colorant.  Use complete pigment system including integral colorants, dry shake colorants, and/or release hardeners from one of the following manufacturers, or other sources as approved by the Engineer.

Brickform	989-792-9009

Decorative Concrete Resources	866-792-9000

Increte Systems	800-752-4626

L.M. Scofield Co.	586-292-1492

Prism Pigments	888-440-4250

Proline Concrete Tools	800-795-4750

A.	Concrete Integral Color.  Use Slate Grey (P9110) for the main pattern and Dolphin (P9120) for the border.  Use pre-weighed and packaged coloring pigments in either powder, granular, or liquid form.  Ensure that materials comply with ASTM C979/C979M standards for integrally colored concrete.

B.	Release Agent.  Use a Dark Gray dry-shake powder to facilitate release of imprinting tools as manufactured by Brickform, Prism Pigments, or approved equal.

2.	Curing Compound.  Do not use standard curing compounds on decorative concrete.  Instead use a surface sealer as listed in subsection d.3 of this special provision.

3.	Surface Sealer.  Use a Type I, Class A solvent acrylic sealer in accordance with the requirements of ASTM C1315 from the approved list below, or other as approved by the Engineer.

A.	Brickform.

●	Safety-Seal MS-5.

B.	ChemMasters.

●	Certi-Vex AC 1315 solvent base sealer.

4.	Slip resistant additive.  Mix slip resistant additive with the sealer in accordance with the manufacturer’s recommendations.

A.	Increte.

●	Shur-Grip.

B.	ChemMasters.

●	Slip Stop.

C.	H & C.

●	SharkGrip.

e.	Equipment.  To impart desired texture, use high-quality resilient mats reproduced from castings of natural materials and furnishing uniform control of joint depth.  Use tools capable of producing the pattern(s) shown on the plans and/or as required by the Engineer.  Use imprinting tool(s) from the approved manufacturer and pattern list below, or present a substitute mat design, manufacturer, or pattern to the Engineer for approval:

Ashlar (TM-100) stamp pattern with Soldier Course Used Brick (FM-5300) stamp pattern border.

f.	Field-Constructed Mock-up.  Prior to installation of colored concrete and/or stamped concrete work, construct mock-up panels in place to verify color and texture selections and processes for qualities of appearance, materials, and construction.  Build mock-ups to comply with the following requirements:

1.	Size.  Cast a minimum 8 foot by 8 foot mock-up to demonstrate typical joints, surface finish, texture, color, and standard of workmanship.

2.	Acceptance.  If Engineer determines that mock-up does not meet requirements, demolish, and remove it from the site, and cast another until the mock-up is accepted.  All costs associated with mock-ups in addition to the first will be borne by the Contractor.

3.	Use.  Keep accepted mock-up undisturbed during construction as a standard for comparison to completed work.  Undamaged mock-up may be incorporated into the work or demolished and removed from the site when directed by the Engineer.

g.	Construction.  Construct sidewalk in accordance with section 803 of the Standard Specifications for Construction.

1.	Preparation.  Carefully lay out the locations of forms and joints, taking into consideration the orientation of the pattern as shown on the plans, intended aesthetics, and construction sequence.

2.	Integral Color.  Comply with the color manufacturer's published recommendations and instructions for mix designs, admixtures, concrete temperature, mixing, installing, finishing, and curing.  Coordinate stamped colored concrete to ensure consistency in color, texture, and quality.

3.	Release Agent.  Apply powder release agent per manufacturer guidelines at the minimum rate required to cover the previously colored surface.  “Liquid Antique” agent can be used as a substitute for the dry release agent.  If clear liquid release agent is to be used, apply per manufacturer guidelines.  Colored powder release agent can be mixed with clear liquid and sprayed on the surface only after the imprinting has been completed, to create an accent coloring.

4.	Imprint Pattern.  Comply with tool manufacturer's standards and MCA practices.  Lay out to proper alignment and imprint to a consistent depth while concrete is plastic.  Do not allow the surface to crust over or harden before stamping.  Hand-tool in areas where using imprinting tools is not practical.

5.	Removal of Excess Release Agent.  Wash off excess release agent with normal water pressure prior to joints being cut.  Remove a minimum of 80 percent of the release agent.  Temperature conditions will dictate the timing of release agent removal.  Dispose of any excess release agent in compliance with local regulations.

Acid washing of decorative surface may be required to achieve the desired finish as directed by the Engineer.  A minimum of 36 hours after placement, apply a solution of 1 part muriatic acid to 30 parts potable water to the surface of the sidewalk and lightly scrub with a straw broom.  Wash the surface until proper color has been achieved and then flush thoroughly.

6.	Sealing Decorative Surface.  Seal the surface with approved sealer in accordance with the manufacturer’s recommendations.  Refer to subsection d.3. of this special provision for approved products and to the manufacturer’s technical data sheets for proper installation procedures, including moisture content restrictions at time of application.

h.	Measurement and Payment.  The completed work, as described, will be measured and paid for at the contract unit price using the following pay item:

Pay Item	Pay Unit

Sidewalk, Conc, Decorative, __ inch	Square Foot

Sidewalk, Conc, Decorative, __ inch includes coloring, mixing, hauling, placement, strike-off, finishing, texturing, stamping, curing and jointing.  Sidewalk, Conc, Decorative, __ inch will be measured and paid for by area in square yards based on plan quantities.