MICHIGAN

DEPARTMENT OF TRANSPORTATION

SPECIAL PROVISION

FOR

SIDEWALK, BRICKWORK

GR:NGJ	1of 3	APPR:TEB:DMG:07-18-22

a.	Description.  This work consists of preparing a concrete base, furnishing and installing a sand bed, and salvaging, furnishing and installing brick pavers (pavers) or removing clay brick pavers and the subbase materials in the areas shown on the plans.  Perform this work with workers with a satisfactory record of performance on completed projects of comparable size and quality.  Provide references to the Engineer if requested.

Review installation procedures and coordinate this work with other contractors or subcontractors working in the area.  Furnish and install temporary barricades and warning lights, as required, for public safety and protection of work.  Protect adjacent work from damage, soiling or staining during paving operations.

b.	Materials.  Furnish materials in accordance with the standard specifications and this special provision.  Store granular materials in a well-drained area on a solid surface to prevent mixing with foreign materials.  Do not use frozen materials or materials mixed or coated with ice or frost.

1.	Pavers.  Salvage pavers free of defects to be reused in the locations shown on the plans.  If additional pavers are necessary, provide red clay brick pavers in accordance with ASTM C902, for Class SX, Type I, Application PS and matching the dimensions of the existing pavers or as directed by the Engineer.  Supply pavers that are uniform in dimension, color, and texture.  Furnish manufacturer's product data and installation instructions for pavers.  The Engineer will visually inspect and approve supplied bricks prior to placement.

A.	Furnish only sound pavers free of defects that could interfere with proper installation or reduce the service life of the finished work.  Minor cracks and minor chipping incidental to methods of manufacture or handling are subject to visual inspection and the Engineer's approval.  Excessive cracks and chips will be cause for rejection.

Ensure there is no efflorescence evident upon visual inspection of the pavers at the project site.

B.	Furnish manufacturer's test data certification, in accordance with the MQAP Manual, documenting that the pavers meet these specifications when tested as specified in ASTM C902.  Conduct freeze - thaw tests not more than 12 months prior to delivery.

If sampling and testing is required, sampling frequency and sample size will be as stated for concrete brick in Section G of the MQAP Manual.

C.	Submit a minimum of five full size samples to the Engineer for review and approval prior to placement.

D.	Protect pavers from damage, chipping and soiling during delivery and storage.  Store off the ground on pallets or wood platforms.  Do not use pavers with chips, cracks, voids, discoloration, or other visible defects exceeding the limits in ASTM C902.

E.	Do not change source of pavers during the course of the work.

2.	Base Material.  Furnish a subbase material in accordance with subsection 301.02 of the Standard Specifications for Construction.  Furnish materials for the 4 inch concrete base course in accordance with subsection 803.02 of the Standard Specifications for Construction.

3.	Leveling Material.  Use 2NS or 2SS fine aggregates in accordance with section 902 of the Standard Specifications for Construction or blast furnace slag sand meeting the gradation shown in Table 1 (commercially known as 30A Blast Furnace Slag):

Table 1:  Grading Requirements for 30A Blast Furnace Slag

| SIEVE ANALYSIS (ASTM C136/C136M) TOTAL PERCENT PASSING |  |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
| U.S. Sieve | 3/8" | #4 | #8 | #16 | #30 | #50 | #100 | #200 |
| % Passing | 100 | 95-100 | 70-95 | 45-75 | 25-55 | 15-35 | 0-20 | - |

4.	Paver Joint Filler.  Use 2MS fine aggregate in accordance with section 902 of the Standard Specifications for Construction.

5.	Edge Restraints.  Paver Units (Soldier Course).  Fill gaps at the edge of the paved surface with standard edge pieces or with paver units cut to fit.

c.	Construction.  Maintain pedestrian and vehicular traffic in accordance with the contract, in the area during installation of pavers.  Do not build on frozen, wet, saturated, muddy, or unstable subgrade.  Protect partially completed paving against weather damage when work is not in progress.  Remove and replace completed work damaged by frost or freezing at no cost to the contract.

1.	Base Course.  Place base course materials only on an approved surface.  Place subbase material in accordance with subsection 301.03 of the Standard Specifications for Construction, except construct the subbase to the required grade and cross section within a tolerance of 1/4 inch.  Construct the 4 inch concrete base course in accordance with subsection 803.03 of the Standard Specifications for Construction and Standard Plan R-29 series, except as modified by the details shown on the plans and this special provision.

2.	Leveling Course.  Spread leveling course material evenly over the entire area to be paved, screed to a level that will provide a minimum 1/2 inch thickness when the pavers are placed and vibrated.  Protect completed leveling course from damage until covered with paver units.  Do not pre-compact leveling course.

3.	Pavers.  Correct any unsatisfactory substrate or installation conditions prior to placing any pavers.  Use full pavers wherever possible.  Where cutting is required, use the largest size pavers possible.  Cut pavers to provide required pattern and to neatly fit adjoining work.  Cut pavers with block splitter or other equipment designed to cut masonry with clean, sharp unchipped edges.  Ragged cuts will not be accepted.  Cut through the full thickness of the pavers.  Do not cut more than 1 inch of the 4 inch dimension of a soldier course.

Lay paver units in the pattern matching adjacent brickwork.  Set all pavers 1/4 inch above existing adjacent concrete curbs and adjoining work.  Maintain uniform 1/16 inch to 1/8 inch joints between pavers.

Vibrate pavers to final grade with three or more passes of a vibratory plate compactor.  After the first pass, brush joint filler material over the surface and vibrate into the joints with additional passes.  Completely fill all joints.  After final vibrating, the surface must be true to grade and not vary by more than 1/4 inch when tested with a 10-foot straightedge at any location on the surface.

Remove and replace pavers that are broken, chipped, stained or otherwise damaged.  Provide new matching pavers, install as specified and to minimize evidence of replacement.

Clean pavers during installation and upon completion of the work.  Repair damage to adjacent areas resulting from paver installation operations, as directed by the Engineer.

Remove and properly dispose of all excess material and debris upon completion of paver installation.

d.	Measurement and Payment.  The completed work, as described, will be measured and paid for at the contract unit price using the following pay items:

Pay Item	Pay Unit

Sidewalk, Brickwork	Square Foot

Sidewalk, Brickwork, Rem	Square Foot

1.	Sidewalk, Brickwork includes completing the work as described herein, including removal, storage and disposal of waste materials in accordance with subsection 205.03.P of the Standard Specifications for Construction is included and will not be paid for separately.

2.	Sidewalk, Brickwork, Rem includes removing all pavers and subbase materials, salvaging existing pavers, and disposal of existing materials in accordance with subsection 205.03.P of the Standard Specifications for Construction.