MICHIGAN
DEPARTMENT OF TRANSPORTATION

SPECIAL PROVISION
FOR

# STEEL GRATING

GLD:MRR	1 of 1	APPR:NAP:SCK:06-15-22

a.	Description.  This work consists of furnishing, fabricating and erecting the proposed steel grating, including but not limited to the steel grid panels, connection angles and fasteners as detailed on the plans, specifications, approved shop drawings and in accordance with manufacturer’s installation standards.

b.	Materials.  Furnish all materials in accordance with section 707 of the Standard Specifications for Construction, except as modified herein.

1.	Use steel grating manufactured by Bailey Bridge, Inc., LB Foster Company, Ohio Grating, Inc. or an approved equal.

2.	Fabricate the steel grating and all components from AASHTO M270M/M270 Grade 36 Steel.

3.	Ensure the steel grating is able to span a minimum of 6 feet, withstanding a pedestrian load of 90 psf with a maximum allowable deflection of 1/1000.

4.	Ensure the steel grating and all components are hot-dip galvanized per ASTM A123/A123M.

5.	Ensure the steel grating has a maximum grid opening of 1/2 inch and includes a traction finish or a serrated top for slip-resistance in wet or dry conditions.

c.	Construction.  Complete all work in accordance with section 707 of the Standard Specifications for Construction, except as modified herein.

Mechanically attach steel grating to the connection angles or channel walls as recommended by the manufacturer and approved by the Engineer.  Shop welding is allowed if specified by the manufacturer, field welding is prohibited on the steel grating.  Alternate attachment methods as proposed by the manufacturer will be considered by the Engineer.  If the alternate attachment methods is approved by the Engineer it will be at no additional cost to the contract.

d.	Measurement and Payment.  The completed work, as described, will be measured and paid for at the contract unit price using the following pay item:

Pay Item	Pay Unit

Steel Grating, Furn and Erect	Square Foot

Steel Grating, Furn and Erect includes furnishing, fabricating, and erecting the steel grating.